## Slide 1
DFT calculation of KF on SiC and Al2O3
C
Si
O
Al
Trigonal, R3m
Trigonal, R3̅c

## Slide 2
Si terminated SiC and KF
1.89718(0) Å
Si terminated SiC
E_SiC_Si =
-635.86651487
KF
2.65441(0) Å
E_KF = -33.71625658/4 = -8.42906

## Slide 3
After adsorption of KF
1.98647(0) Å
1.64059(0) Å
Etot = -645.35468814
DFT calculation on adsorption of KF on Si layer on SiC
Adsorption energy:
Ead = Etot - E_SiC_Si - E_KF = -1.05898

## Slide 4
KF
2.65441(0) Å
C terminated SiC
With fixing the nearest Si layer
C terminated SiC
Without fixing the nearest Si layer
DFT calculation on adsorption of KF on C layer on SiC
1.90327(0) Å
1.98716(0) Å
E_SiC_C = -675.693
E_KF = -33.71625658/4 = -8.42906

## Slide 5
After adsorption of KF
1.49067(0) Å
Adsorption energy:
Ead = Etot - E_SiC_Si - E_KF = -0.30545
Etot = -684.427
Chart: Adsorption energy / eV
| Adsorption energy of KF on SiC_Si | Adsorption energy of KF on SiC_C
 | -1.059 | -0.30545
DFT calculation on adsorption of KF on C layer on SiC
-1.05898
Si-F prefers to be formed than C-F

## Slide 6
Al terminated Al2O3 and KF
Al terminated Al2O3
E_Al2O3_Al = -442.854
KF
2.65441(0) Å
E_KF = -33.71625658/4 = -8.42906

## Slide 7
Adsorption energy:
Ead = Etot - E_Al2O3_Al - E_KF = -0.90743
E_tot = -452.191
Al terminated Al2O3 and KF
K-O
F-Al

## Slide 8
O terminated Al2O3
E_Al2O3_O = -463.578
KF
2.65441(0) Å
O terminated Al2O3 and KF
E_KF = -33.71625658/4 = -8.42906

## Slide 9
Chart: Adsorption energy / eV
| Adsorption energy of KF on Al2O3_Al | Adsorption energy of KF on Al2O3_O
 | -0.90743 | -6.3239
O terminated Al2O3 and KF
Adsorption energy:
Ead = Etot - E_Al2O3_Al - E_KF = -6.32389
E_tot = -478.331
K-O

## Slide 10
Adsorption energy of KF – SiC and KF – Al2O3
O – K, Si - F, Al - F

## Slide 11
Electron configurations between Si-F
K
F
Si
F
Si
Ionic bonding
Covalent Bond

## Slide 12
Electron configurations between K-O and F-Al
Al-F
K-O
All ionic bond

## Slide 13
Electron configurations between K-O
K-O
K
F
O

## Slide 14
HOMO-LUMO